## Slide 1
Exploring Solution Plasma Sprayed Coating Architectures for CMAS Resistance

## Slide 2
Significant problems with feeding fine powders are obviated
A fair bit is now “known”, but much is still in the realm of conjecture / mystery … so vast areas remain to be explored
It is very inter-disciplinary, e.g., chemistry inputs especially vital, than at any other time in thermal spray history
Novel coating chemistries conveniently possible
There can be life beyond TBCs for solution plasma spraying … relevant for many other applications
Solution plasma spraying: Why should it capture our imagination?

## Slide 3: Why now ?
Axial Injection
Injection into the centre of the plasma, coaxial to plasma flow
Less sensitive to suspension properties and injection parameters
Radial Injection
Injection in plasma plume periphery, 60°-90° to flow
Injection parameters require tuning and are sensitive to suspension parameters
Axial feeding particularly ideal for solution feedstock; more effective utilization of plasma energy, capable of better addressing concerns of reduced productivity
Axial feed, high power plasma spray systems are game changers

## Slide 4
Deposition Efficiency: SPS vs. SPPS,
effect of plasma power & spray distance
M.Marr et al., J. Power Sources, 245 (2014) 398
Many interesting observations:
High deposition efficiencies achievable with solution-based precursors
Plasma power & spray distance can play a dominant role
Particularly in case of solution precurors – beyond certain threshold power level, DE for solution precursors can be attractive
Dramatic drop in DE at very high spray distance indicative of resolidification prior to impact

## Slide 5
Axial Suspension Plasma Sprayed
Gadolinium Zirconate-based TBCs for Combating CMAS Attack

## Slide 6
Lower thermal conductivity than YSZ
Excellent phase stability
Better CMAS attack resistance than YSZ
Why Double layer GZ/YSZ?
GZ has a lower fracture toughness than the conventionally used 8YSZ
GZ also reported to react with alumina (TGO) at high temperature, leading to formation of GdAlO3
Therefore, GZ/YSZ double layered TBCs with 8YSZ as the intermediate layer appears more promising
Why Gadolinium Zirconate?
Vassen et al. ‘Overview on advanced thermal barrier coatings’ Surf. Coat. Technol., Vol. 205, 2010

## Slide 7
Why Suspension Plasma Spray (SPS)???
Courtesy, N.P. Padture et al, Ohio State university
APS Microstructure
EB-PVD Microstructure
Courtesy, S. Mahade et al., 2015, University West
SPS Microstructure
SPS mimics EB-PVD to generate a columnar microstructure and also yields a lower thermal conductivity
Courtesy, N. Curry et al, University west
High strain tolerance
Low thermal conductivity

## Slide 8
Suspension plasma spraying (liquid feedstock)
Feedstock | Suspension (Liquid feedstock)
Powder particle size | Finer ( < 1µm)
Coating microstructure | Fine structured & Columnar (can be altered based on parameters)
Process Characteristics
Cross sectional SEM micrograph of SPS deposited TBC
Schematic of the axial SPS process

## Slide 9
Coating architectures investigated
Improve Erosion resistance
Improve CMAS infiltration resistance

## Slide 10
Single layer YSZ a)Cross section b) Top view
Double layer GZ/YSZ a)Cross section b) Top view
Columnar microstructures could be generated in both single and double layer TBCs

## Slide 11
Triple layer GZdense/GZ/YSZ a) Cross section b) Top view
Relatively dense top layer through suitable spray parameter control (different D50 of the solute)

## Slide 12
1 wt.% Hekla, YSZ single layer
Ash
YSZ single layer TBC showed no horizontal cracks upon exposure to Hekla ash
However, infiltration (?) through the intercolumnar spacing is feared and prospects for long life with such a single-layer, columnar coating architecture did not appear encouraging

## Slide 13
1 wt.% Hekla, GZ/YSZ double layer
Horizontal crack
GZ/YSZ double layer TBC showed horizontal cracks in the GZ layer close to the interface with YSZ
Reason for crack propagating through GZ layer instead of YSZ is due to the lower fracture toughness of GZ than YSZ (approximately double than GZ)
Further investigations need to be made to find the reason for the origin of horizontal crack in double layer TBC

## Slide 14
1 wt.% Hekla, GZdense/GZ/YSZ triple layer
Horizontal crack
Spallation of denser GZ
GZ dense/GZ/YSZ triple layer TBC also showed horizontal cracks in the 2nd GZ layer, but closer to the columnar/dense GZ coatings’ interface
Further investigation ongoing to explain these observations
Also, repeat experiments and explore alternate coating architectures

## Slide 15
As sprayed TBCs exposed in ambient air at 1150ºC (No ash added on top)
GZdense/GZ/YSZ
GZ/YSZ
With no ash, the TBCs did not show presence of any horizontal cracks, although the exposure time was much longer at an identical test temperature

## Slide 16
Al2O3/YSZ (60µm APS /280µm SPS)
Alumina (APS) 60 µm
YSZ (SPS) 280 µm
Bond coat
Substrate
Al2O3/YSZ, Hekla ash@1150ºC, 1 hour

## Slide 17
Alumina
YSZ
Ash
Vertical crack opening
1 wt.% Hekla @1150ºC , Al2O3/YSZ (60µm APS /280µm SPS)
60 µm thick alumina layer deposited by APS process on SPS deposited YSZ
Motivation to deposit the thin alumina layer by APS was to seal the columns formed in YSZ and beside providing additional protection

## Slide 18
Future Plans
CMAS test of the GZ based multilayered TBCs are planned under a burner rig … this work is being carried out in collaboration with FZ Julich, Germany
Explore different top coat compositions for added CMAS protection (yttria / YAG / alumina)
Evaluate different TBC “designs”

## Slide 19
Improvements in
Gas Turbine Performance via
Novel Plasma Spray Coatings Offering Protection Against Ingested Species
Under
DST-EPSRC Research Initiative on Advanced Manufacturing

## Slide 20
Choice of feedstock
Gd2Zr2O7 coatings known to be effective against CMAS - form easy-to crystallize Ca2Gd8(SiO4)6O2 apatite phase
Relatively lower ionic sized Y3+ based materials that favour formation of Ca4RE6(SiO4)6O make choice of Y2Zr2O7 interesting
La2Ce2O7 is stable @ 1400°C with low thermal conductivity (0.5‒1.02 W/mK at 1473 K), high CTE (12.3‒12.6 x 10-6/K at 573‒1473 K) than YSZ (2.1 W/mK, 10.5‒11.5 x 10-6/ K)
Addition of relatively smaller ionic radii, Gd3+ to La2Ce2O7 to form (La1−xGdx)2Ce2O7 is expected to accelerate crystallization of Ca4RE6(SiO4)6O phase and also reduce low temp CTE

## Slide 21
Preparation of feedstock for APS & SPPS
Thermal spray grade Gd2Zr2O7 powders are available as proprietary; Y2Zr2O7 is also a commercially available TS grade powder
La2Ce2O7 and (La1−xGdx)2Ce2O7 are not available as standard TS grades and were synthesized in-house through arc melting and solid state sintering, respectively
Coatings of similar chemistry can be generated through SPPS using formulated precursors

## Slide 22
Synthesis of La2Ce2O7 & La1.8Gd0.2Ce2O7
CeO2
(2mole)
La2O3
(0.9mole)
Gd2O3
(0.1mole)
Milling-Zirconia balls,
Isopropanol medium, 7hrs
Dried at 60-70°C
Sintered at 1600°C
4hrs
Cubic fluorite La1.8Gd0.2Ce2O7
Spray grade powders
APS
coatings
+
CeO2
(2mole)
Ball milling
Corundum jar and ball
4hrs
La2O3
(1mole)
Compaction to make pellets
Plasma transferred
arc melting (PTA)
Cubic fluorite La2Ce2O7
Planetary ball mill
Binder (PVA) and lubricant (Stearic acid)
Milled powder
Pellets
Cakes of La2Ce2O7
APS
coatings
Spray grade powders
Crushed & Sieved
Crushed & Sieved

## Slide 23
Gd2Zr2O7*
Y2Zr2O7
La2Ce2O7
La1.8Gd0.2Ce2O7
Y2O3
Y2Zr2O7
162.2 g Y(NO3)3.6H2O +194.38ml Zr(CH3COO)4
Gd2Zr2O7
147.8 g Gd(NO3)3.6H2O +152.24ml Zr(CH3COO)4
Y2O3
339.2g Y(NO3)3.6H2O
La2Ce2O7
129.2g La(NO3)3.6H2O + 129.61g Ce(NO3)3.6H2O
La1.8Gd0.2Ce2O7
115.6g La(NO3)3.6H2O + 128.9g Ce(NO3)3.6H2O
13.4 g Gd(NO3)3.6H2O
Powder
Solution precursor
Candidate feedstock materials
Commercial grades
* - Proprietary
In-house synthesis

## Slide 24
Processing route
Deposition of RE zirconates directly over conventional bond coats yielded poor thermal cyclic performance due to low CTE (relative to BC), low toughness values and reactivity with TGO (formation of LaAlO3 while applying La2Ce2O7 over BC)
Double layered structure (top coat = REO + YSZ) is being evaluated
Composite APS + SPPS microstructure also being explored to improve CTE and toughening
Substrate
Atomizer
Plasma gun
Pressurized
precursor tank
Coating
Atomized
droplets
Powder
Powder
injector
Top coat- APS/SPPS
Substrate
Top coat- APS
Bond coat
Top coat-SPPS+APS
Substrate
Bond coat

## Slide 25
Tasks accomplished so far
Optimization of process parameters for candidate feedstock materials - powders and solution precursors
Deposition of layered coatings comprising a CMAS resistant layer over conventional YSZ
Deposition of composite coatings involving CMAS resistant materials along with solution derived n-YSZ
Performance testing with CMAS –In progress

## Slide 26
Plasma spraying of on Gd2Zr2O7 : Parametric impact
500A
550A
600A
650A
Plasma power significantly influences the porosity, but not so much the phase content

## Slide 27
Optimized microstructures for CMAS resistant materials
APS
Solution precursor
Gd2Zr2O7
Y2Zr2O7
La2Ce2O7
La1.8Gd0.2Ce2O7
Y2O3
La2Ce2O7
Y2O3
Gd2Zr2O7
Y2O3-ZrO2
Detailed optimization based on phase contents and microstructural features
All powder based coatings were optimized
Formulation of precursor based on stoichiometry and concentration

## Slide 28
Y2Zr2O7
YSZ
NiCoCrAlY
Double layer APS Y2Zr2O7-YSZ
Thick layers of optimized RE zirconate deposited over YSZ on bond coated C263 substrate
Top layer exhibits the preferred phase and expected to provide resistance to CMAS
Interlayer compatibility between the top coat layers
Y2Zr2O7
YSZ
YSZ
NiCoCrAlY

## Slide 29
Double layer APS Gd2Zr2O7-YSZ
Gd2Zr2O7
YSZ
NiCoCrAlY
Gd2Zr2O7
YSZ
NiCoCrAlY
Gd2Zr2O7
YSZ
Single phased top layer of Gd2Zr2O7 is known for the CMAS resistance
Interlayer compatibility between the top coat layers

## Slide 30
La2Ce2O7
YSZ
NiCoCrAlY
Double layer APS La2Ce2O7-YSZ
In-house synthesized La2Ce2O7 with acceptable TBC characteristics shown good coatability as single or double layer

## Slide 31
La1.8Gd0.2Ce2O7
YSZ
NiCoCrAlY
Double layer APS La1.8Gd0.2Ce2O7-YSZ
La1.8Gd0.2Ce2O7
YSZ
La1.8Gd0.2Ce2O7
YSZ
NiCoCrAlY
In-house synthesized La1.8Gd0.2Ce2O7 also shown good coatability as single or double layer
Effectiveness against CMAS is under evaluation

## Slide 32
Development of Hybrid TBCs-Coating formation
Involves simultaneous injection of powders and solution precursor salts to form micron-sized powder and nanostructured features respectively, within the microstructure
Possibility of improved toughness, increase of CTE can be achieved with bimodal type of microstructures deposited through hybrid processing
Composite coatings prepared include Gd2Zr2O7+ YSZ (S), Y2Zr2O7 + YSZ (S), La2Ce2O7 + YSZ (S), La1.8Gd0.2Ce2O7 + YSZ (S) coatings
JTST, 24 (7), 1166-1186, 2015

## Slide 33
Composite Gd2Zr2O7+YSZ
Composite Gd2Zr2O7(P)+YSZ(S)
Introduction of nYSZ in composite Gd2Zr2O7(P)+YSZ(S) improved the coating hardness as well as toughness

## Slide 34
Composite Y2Zr2O7+YSZ
Coatings with controlled porosity can be deposited

## Slide 35
Composite (LaxGd1-x)2Ce2O7+YSZ
Optimized the composite coatings of (LaxGd1-x)2Ce2O7+YSZ with dual phase of fluorite and t’-ZrO2

## Slide 36
CMAS performance testing
Thermal cyclic studies with CMAS @ 1150oC for various layered and composite coatings is in progress
Based on the preliminary evaluation, layered coatings of (LaxGd1-x)2Ce2O7-YSZ, Y2Zr2O7 – YSZ and Gd2Zr2O7 – YSZ appear to show relatively better resistance to spallation

## Slide 37
CMAS performance testing with DL SPPS REO-APS YSZ
Layered SPPS La2Ce2O7-APS YSZ
Coating survived without any spallation after 10 cycles without any significant increase in density within YSZ layer
The layer of La2Ce2O7 observed to prevent the infiltration of CMAS
Thermal cycled at 1150°C for 10 hrs (10 cycles) with Laki volcanic ash loading of 4 mg/cm2

## Slide 39
Hekla Ash @ 1150ºC exposed for 1 hour (isothermal treatment)
YSZ
GZ/YSZ
GZ dense/GZ/YSZ

## Slide 40
Porosity measurement of the as sprayed TBCs
Porosity content of the as sprayed TBCs was measured using 2 methods
Porosity values of the TBCs lie in the range of 18-22 Vol.%

## Slide 41
XRD of the as sprayed TBCs
XRD analysis of GZ based TBCs showed a cubic defect fluorite structure
In the case of YSZ, a tetragonal prime phase was observed